Analysis of Slack Wax 5% oil content

| Characteristic | Unit | Typical | Test method |
| --- | --- | --- | --- |
| Kinematic viscosity @100 ˚C | Cst | 5 | ASTM D-445 |
| Flash point | ˚C | 230 | ASTM D-92 |
| Specific gravity 25 ˚C/25 ˚C | – | 0.8 | ASTM D-190 |
| Oil Content | %wt | 3-5 | ASTM D-721 |
| Congealing Point | ˚C | 55 | ASTM D-937 |
| Color | – | 3 | ASTM D-1500 |
| Drop Melting Point | ˚C | 57 | ASTM D-127 |