Analysis of Slack Wax 12% oil content

| Characteristic | Unit | Typical | Test method |
| --- | --- | --- | --- |
| Kinematic viscosity @100 ˚C | Cst | 7 | ASTM D-445 |
| Flash point | ˚C | 250 | ASTM D-92 |
| Specific gravity 25 ˚C/25 ˚C | – | 0.82 | ASTM D-190 |
| Oil Content | %wt | 12 | ASTM D-721 |
| Congealing Point | ˚C | 50 | ASTM D-937 |
| Color | – | YELLOW | ASTM D-1500 |
| Drop Melting Point | ˚C | 50 | ASTM D-127 |