

**Analysis of Slack Wax 12% oil content**

|  |  |  |  |
| --- | --- | --- | --- |
| **Characteristic** | **Unit** | **Typical** | **Test method** |
| **Kinematic viscosity @100 ˚C** | **Cst** | **7** | **ASTM D-445** |
| **Flash point** | **˚C** | **250** | **ASTM D-92** |
| **Specific gravity 25 ˚C/25 ˚C** | **–** | **0.82** | **ASTM D-190** |
| **Oil Content** | **%wt** | **12** | **ASTM D-721** |
| **Congealing Point** | **˚C** | **50** | **ASTM D-937** |
| **Color** | **–** | **YELLOW** | **ASTM D-1500** |
| **Drop Melting Point** | **˚C** | **50** | **ASTM D-127** |